Любименко Е.Н., Гольцова М.В. Формирование градиентного Pd-H сплава и формоизменение палладиевой пластины при одностороннем насыщении водородом // Металлофизика и новейшие технологии. – 2011. – Т. 33. – № 6. – с. 819–829.

Аннотация: Создана новая водородно-вакуумная установка для исследований формо-

изменений палладиевой пластины при её одностороннем насыщении водо-

родом при температурах выше 110C. Исследования выполнены при 240C

в широком интервале давлений. Установлено, что при водородном воздей-

ствии обратимые изгибы палладиевой пластины достигают величин, при-

мерно в 2,5 раза больших, чем обратимые изгибы при чисто механическом

нагружении. Обсуждены физические причины и сделан вывод о природе

изучаемого явления, состоящей в формировании временного градиентного

когерентного сплава PdHx при насыщении металла водородом.

------------------------------------------------------------------------------------------------

M. V. Gol’tsova and E. N. Lyubimenko, Effect of Temperature on the Form Change of a Palladium Plate during Its One_Sided Saturation with Hydrogen. Physics of Metals and Metallography, 2012, Vol. 113, No. 2, pp. 153–159.

Abstract—Effect of temperature on the regularities and scale of form changes of a palladium plate has been studied in a cantilever mode of fixation of a specimen, during its one_sided saturation with hydrogen. The form change of the plate is confirmed to be developed in two stages. During the first short_time stage, the maximum form change (bending) of the plate is reached. The temperature dependence of the maximum bend of the plate is described by an extremal function. During the second stage, which is of substantially longer duration, a plate straightening takes place. At low temperatures, the residual steady_state bend of the plate is 20–30% of the maximum form change. As the temperature increases, the bend reversibility increases and at 320–350°C the phenomenon becomes completely reversible. The mechanism of form change is discussed, and its phenomenological analysis is given.

----------------------------------------------------------------------------------------------